## Slide 1
PMD Material Data Set 42CrMoS4
Process Schema
  —
    M. Luke, 04.12.2025

## Slide 2: PMD Material Data Set
1 bar= 1 tensile specimen+1 metallographic specimen
Material batches:
  T 850  Charge 3466
  T 925  Charge 3467
  T 1000  Charge 3468
  T 1150  Charge 3470
  T 1075  Charge 3471
      Process Schema
Hardness measurement HV 10 (IWM)
Met. sample
5 material batches!
Shipping
(IWT2IWM)
Separation
(IWT)
IRAN-Steel: 42CrMoS4
Quenched and tempered
Heat Treatment
(IWT)
…
Heat treated bars:
Hardened and tempered
kept as
reference
…
Separation
(IWM)
…
Separated bars
ID=1,2, …
70 bars
ID= 1,2, …
Kept by IWT
Tensile test
(IWM)
Spectroscopy
(IWT)
Grain size measurement (IWT)
Separation
(IWT)
Met. sample
Hardness measurement
HV 10 (IWT)
Metallographic preparation (IWM)
Met. sample
Hot rolled piece
ID=1,2, …
IWM-Label
IWT-Label
Met. sample
Shipping (IWM2IWT)
Polished again
70 tensile test specimens
70
70
Met. sample
Hardness measurement
HV 1 (IWM)
LiMi+Grain size evaluation
(IWM)
Met. sample
IWM-Label
IWM-Label
IWM-Label
IWM-Label
IWT-Label
IWM-Label
…
IWM-Label
70 metallographic specimens
Block to be digitalized by IWT!
Roughness measurements
(IWM)
Notes: HeatTreatment: position in oven attached via picture file
Hardening and tempering modelled in two separated graphs